## Slide 1: Ultra-high purity electroforming for rare event searches P. Knights1, K. Nikolopoulos1,2, G. Rogers1, D. Spathara1, P. Walters1 1University of Birmingham, 2University of Hamburg

## Slide 2
Copper as a detector material
Copper is a common detector material for rare event searches
  Commercially available at high-purity up to high-purity
  Good mechanical and electrical properties
  No long-lived radio-isotopes
CUORE collaboration
https://cuoreexperiment.org
NEWS-G collaboration
https://www.snolab.ca/experiment/news-g/

## Slide 3
Copper background
Copper can still represent an important background
Commercial copper contaminated - 238U and 232Th decay chains:
  Natural ore contamination
  Cosmogenic activation
  Implanted during manufacture
Simulated backgrounds for NEWSG’s current detector
238Ur decay chain

## Slide 4
Electrodeposition
Deposit Cu2+ ions onto a cathode by applying a voltage
Copper has a higher reduction potential than contaminants -> more easily reduced onto the cathode
Electroplating
Electroforming
Cu plated onto existing structure (i.e. cryostat) acting as an ultra-pure shield
Cu plated onto a mould (called mandrel)
Remove the mandrel leaving a pure copper structure

## Slide 5
Electrodeposition
Sample of copper | 232Th [uBq/kg] | 238Ur [uBq/kg]
Commercial C10100 | 8.7 ± 1.6 | 27.9 ± 1.9
NEWS-G plated NIMA 988 (2021) 164844 | <0.24 | <0.11
Majorana demonstrator electroformed NIMA 828 (2016) 22-36 | <0.119 | <0.099
NEWS-G electroplated Cu
NIMA 988 (2021) 164844
Majorana demonstrator
Electroformed Cu
OSTI (2012) 1039850
Electroplating
Electroforming
Cu plated onto existing structure (i.e. cryostat) acting as an ultra-pure shield
Cu plated onto a mould (called mandrel)
Remove the mandrel leaving a pure copper structure
Deposit Cu2+ ions onto a cathode by applying a voltage
Copper has a higher reduction potential than contaminants -> more easily reduced onto the cathode

## Slide 6
Recirculating filters
Electroforming facility at Boulby
1.1km underground at the UK’s deep underground laboratory Boulby -> reduce cosmogenic activation
Construction and cleaning finished
Currently commissioning with cylindrical mandrels
Immediate goal: electroform a ⌀30cm SPC DarkSPHERE-30
Ultimate goal: DarkSPHERE 𝒪[⌀3m]
Steel cylindrical mandrel
5.5N Cu feedstock
Cu bus bar
Inlets
CuSO4 electrolyte
Boulby underground lab
https://www.boulby.stfc.ac.uk/Pages/home.aspx
Electroforming bath at Boulby
Ti anodes

## Slide 7
Copper plated onto stainless steel cylinder
Peeled copper off mandrel -> assay results pending
Commissioning

## Slide 8
Physics Potential
Fully electroformed SPCs will have world leading sensitivity to low-mass dark matter
DarkSPHERE-30 will begin construction in the coming months
Alloys being explored to improve the properties of electroformed copper – PureAloys project
  NIMA 1082 (2026) 170970
  arXiv.2507.00799

## Slide 9
Summary
Copper electroforming for radio-pure detectors
Electroforming facility constructed at Boulby
First copper plated onto stainless steel cylinder
Electroforming a ⌀30cm SPC in the coming months
Many other experiments exploring the use of electroformed Cu

## Slide 10
BACKUP SLIDES

## Slide 11
Spherical proportional counter
Proportional counter filled with gas
Choice of gas -> kinematic matching
Low capacitance -> Single electron detection
Simple design -> Radiopure construction
Optimised for light dark matter searches
NewsG operate several SPCs – current detector is Snoglobe at Snolab
JAIS 2025 (2025) 548